Synthesis and characterization of PbS nanoparticles in an ionic liquid using

single and dual source precursors

Zikhona Tshemese, Malik Dilshad Khan, Sixberth Mlowe, Neerish Revaprasadu

Department of Chemistry, University of Zululand, Private Bag X1001, Kwa-Dlangezwa 3886, South Africa

Abstract

We report a green route for the synthesis of PbS nanoparticles in an imidazolium based ionic liquid (IL) (1-ethyl-3-methylimidazolium methanesulfonate) using single source and dual source precursor methods. Lead ethyl xanthogenate complex was used as single source molecular precursor for the synthesis of PbS nanoparticles, whereas in dual source approach organic sulfur (1-dodecanethiol) and inorganic sulfur (sodium sulfide) sources were used to observe the suitability of different sulfur sources on formation of PbS nanoparticles. The results showed that the temperature has an effect on the as prepared nanoparticles for both routes. X-ray diffraction (XRD) studies confirmed formation of cubic phase of PbS from both routes. Electron microscopy techniques showed that the nanoparticle morphologies differed significantly depending on the synthetic factors such as temperature, nature of precursors and ranged from spherical to cubic shapes.

## Keywords

Lead ethyl xanthogenate, Ionic liquid, 1-Ethyl-3-methylimidazolium methanesulfonate, PbS, Single source precursor